## Slide 1
Lecture 6
Junction characterisation
Jon Major
Nov 6th 2014

## Slide 2
The PV research cycle
L6
Make cells
Measure cells
Despair
Repeat
Data

## Slide 3
Lecture Outline
LX
Analysis of current voltage (J-V) curves
External quantum efficiency (EQE) measurements
Capacitance voltage (C-V) measurements
Key junction characterisation techniques

## Slide 4
J-V analysis (J-V)
L6
Parasitic resistances
Perfect p-n junction
Real p-n junction
A good device should have low RS
And high RSh

## Slide 5
J-V analysis (J-V)
L6
Rs
Rsh
Causes of high RS values
Overly thick absorber layer
Low conductivity TCO
Low doping levels
Causes of low RSh values
Pinholes in layers
Weak diode regions

## Slide 6
J-V analysis (J-V)
L6
Rs
Rsh

## Slide 7
J-V analysis (J-V)
L6
To determine Rsh fit to straight line portion of JV curve in reverse bias
Rs can be more difficult to accurately determine. Two common methods
Fit to forward bias region of curve
Measure change as function of light bias
A
B

## Slide 8
J-V analysis (J-V)
L6
“Roll-over”
If a non-ohmic contact is formed this results in the creation of a back contact junction diode.
This back-contact diode opposes the main junction diode and leads to the phenomenon of “roll-over” at high forward bias.

## Slide 9
J-V analysis (J-V)
L6
For a p-type semiconductor can create an ohmic contact if;
Schottky barrier
Ohmic contact
If this condition is not met we introduce a back contact Schottky barrier
Electron affinity
Bandgap
Metal work function
Back contact barrier height

## Slide 10
J-V-T analysis
L6
Influence of barrier height changes as a function of temperature
By measuring J-V curves as a function of temperature we can extract the barrier height
This back-contact diode opposes the main junction diode and leads to the phenomenon of “roll-over” at high forward bias.

## Slide 11
J-V-T analysis
L6
If a non-ohmic contact is formed this results in the creation of a back contact junction diode.
Fitting to exponential region allows us to extract a value in eV for the barrier height. Generally anything < 0.3eV is considered a good contact
Measure RS
Series resistance varies with temperature via
Ohmic resistance
Ohmic temperature
dependence

## Slide 12
A cautionary tale
L6

## Slide 13
Errors in J-V analysis (J-V)
L6
High Voc and FF are reliable
Jsc values are very sensitive to calibration or contact size errors
Contacts should be minimum of 0.25cm2
If it looks to good to be true it usually is!

## Slide 14
External quantum efficiency (EQE)
L6
n-type CdTe
p-type CdTe
n-type CdS
Junction position
Glass/ TCO

## Slide 15
External quantum efficiency (EQE)
L6
Absorber layer (e.g. CdTe)
Window layer (e.g. CdS)
Glass
Transparent conductive oxide (e.g. ITO)
AM1.5
AM1.5
JSC

## Slide 16
External quantum efficiency (EQE)
L6
Define the EQE as the ratio of photons in to current generated
A 100% EQE means every photon that strikes the cell generates an electron hole pair which flows through the external circuit

## Slide 17
External quantum efficiency (EQE)
L6
Theoretical case
Area under curve proportional to JSC

## Slide 18
External quantum efficiency (EQE)
L6
Most solar cell technologies display same typical “top hat” EQE curve shape

## Slide 19
External quantum efficiency (EQE)
L6

## Slide 20
External quantum efficiency (EQE)
L6
Absorber layer (e.g. CdTe)
Window layer (e.g. CdS)
Glass
Transparent conductive oxide (e.g. ITO)
J=0
Region 1: Ephoton<EAsorber

## Slide 21
External quantum efficiency (EQE)
L6

## Slide 22
External quantum efficiency (EQE)
L6
Absorber layer (e.g. CdTe)
Window layer (e.g. CdS)
Glass
Transparent conductive oxide (e.g. ITO)
J≠0
Region 2: Ephoton>EAsorber

## Slide 23
External quantum efficiency (EQE)
L6

## Slide 24
External quantum efficiency (EQE)
L6
Absorber bandgap

## Slide 25
External quantum efficiency (EQE)
L6
Absorber layer (e.g. CdTe)
Window layer (e.g. CdS)
Glass
Transparent conductive oxide (e.g. ITO)
J=0
Region 3: Ephoton>Ewindow

## Slide 26
External quantum efficiency (EQE)
L6

## Slide 27
External quantum efficiency (EQE)
L6
Window bandgap

## Slide 28
External quantum efficiency (EQE)
L6
Real cells

## Slide 29
External quantum efficiency (EQE)
L6
Optical losses
Uniform reduction in EQE signal across wavelength range is an indication of optical losses i.e. reflection loss, optical blockages etc.
Can also be an indication of poor system calibration.
High efficiency
Low efficiency

## Slide 30
External quantum efficiency (EQE)
L6
window/ n-type layer losses
Reduced window layer thickness allows more light transmission to absorber
Higher bandgap n-type layer shifts absorption edge
High efficiency
Lower efficiency
High efficiency
Lower efficiency

## Slide 31
External quantum efficiency (EQE)
L6
If absorber layer is thin or depletion width is narrow then longer wavelength photons have an increased probability of not contributing to photocurrent. See a decrease in EQE for longer wavelengths.
Deep penetration losses

## Slide 32
External quantum efficiency (EQE)
L6
In multi component materials such as CZTS can get a broad cut-off region due to changes in the absorber bandgap.
This often signifies the material isn’t single phase and reduces the efficiency.
Can also indicate enhanced recombination close to the back surface.
Graded bandgap/back surface recombination

## Slide 33
External quantum efficiency (EQE)
L6
In certain situations see a complete change in EQE that corresponds to very low performance
See reasonable EQE response near absorber band-edge but low response at all other wavelengths

## Slide 34
External quantum efficiency (EQE)
L6
This is a buried junction response due to both p and n type regions being present in the absorber layer

## Slide 35
Capacitance Voltage analysis (C-V)
L6
Capacitance-voltage measurements are useful in deriving particular parameters about PV devices.
Depending on the type of solar cell, capacitance-voltage (C-V) measurements can be used to derive parameters such as the doping concentration
and the built-in voltage of the junction.
A capacitance-frequency (C-f) sweep can be used to provide information on the existence
of traps in the depletion region.
Liverpool CV/Admittance spectroscopy system

## Slide 36
Capacitance Voltage analysis (C-V)
L6
Field
distribution
Space charge
distribution
Can define the junction capacitance per unit area as
Where W is the width of the depletion region and εS is the semiconductor permittivity
Can treat a p-n junction as a capacitor - depletion region sandwiched between two plates.

## Slide 37
Capacitance Voltage analysis (C-V)
L6
We generally assume a one sided abrupt junction for calculations. This is due to the higher doping densities in the n-type layer meaning the depletion region lies within the p-type layer
For a one sided junction we can determine the depletion width as
Acceptor doping density
Electron charge
Using previous equation we get the relation
Hence we can get Na from a plot of 1/C2 vs V

## Slide 38
Capacitance Voltage analysis (C-V)
L6
Measure the capacitance response of the cell as a function of applied bias.
C-V measurements can be made either forward-biased or reverse biased. However, when the cell is forward-biased, the applied DC voltage must be limited; otherwise non-ohmic back contacts can alter the signal.
Worked example – CdTe solar cell
Determine gradient of straight line fit around V=0
C vs. V plot
1/C2 vs. V plot

## Slide 39
Capacitance Voltage analysis (C-V)
L6
So for a CdTe cell with 5mm diameter square contacts we measured a the slope of the 1/C2 plot to be 2.7x1017.
So CdTe doping density is
p-type doping density is given by
We have included a contact area term A

## Slide 40
Summary
LX
JV – RS and RSH  can infer the issue
J-V-T – Back contact barrier height measurements
EQE – Layer behaviour and optical losses
CV - doping density of p-type layer
Key junction characterisation techniques