## Slide 1: Lecture: Solar cell technologies, world records and some new concepts

## Slide 2: Review papers on PV … there are lots
“Materials Today” 2007

## Slide 3: NREL efficiency chart – one of a kind cells
http://www.nrel.gov/ncpv/images/efficiency_chart.jpg
Download the latest version for your work!

## Slide 4: Progress in PV Efficiency Tables

## Slide 5: World Record Cells (and sub-modules)
Criteria for inclusion
(cells):
Independently measured by a recognised test center elsewhere
Area > 1cm2 (= total area!) for one sun devices
Other rules for mini-modules and concentrators
Categories
Silicon
III-V
Thin film
Perovskite / dye
Organic
Multi-junction

## Slide 6: World Record Cells

## Slide 7: Purification of silicon
98% pure Si
HCl
SiHCl3
Distil
Heat under H2
Pure Si
Grow crystal
Or cast ingot
Begin PV
production
http://www.microchemicals.com/products/si_wafers/from_quartz_sand_to_silicon_wafers.html
http://www.tomshardware.com/reviews/semiconductor-production-101,1590-3.html
http://www.resonancegroupusa.com/forum/index.php?topic=40.0
http://www.solarworld.de/fileadmin/sites/sw/presse/bildmaterial/produktion/kristallisation_01_download.jpg
http://cnx.org/content/m31994/latest/
Sand

## Slide 8: Silicon – the world leader
http://www.ubergizmo.com/2011/10/silevo-hybrid-solar-cell-challenges-conventional-wisdom/

## Slide 9: Si – large scale production

## Slide 10: Silicon - crystalline

## Slide 11: Silicon’s best – the Sanyo ‘HIT’ cell
http://us.sanyo.com/News/SANYO-Develops-HIT-Solar-Cells-with-World-s-Highest-Energy-Conversion-Efficiency-of-23-0-
‘Heterojunction with Intrinsic Thin layer’

## Slide 12: Silicon - crystalline
Pic from
Miles 2007

## Slide 13: Silicon – multi-crystalline
Advantages
Cheaper than wafer silicon
Uses silicon processing technology
Disadvantages
5% less efficient than single crystal
(Highest efficiencies need exotic processing (left))
Ref 24 Shultz 2004

## Slide 14: Silicon – multi-crystalline
Pic from
Miles 2007

## Slide 15: III-V
Ref 24 Kayes 2011

## Slide 16: III-V
Ref 24 Kayes 2011

## Slide 17: Thin film - CIGS
Strengths
High efficiency ~ 20%
Thin film construction
Issues
Complex material – chalcogen loss
In and Ga rare and expensive
Business hard to sustain – danger of it being undercut
Image from NREL

## Slide 18: Thin film - CIGS
From ref 27 Repins 2008

## Slide 19: Thin film - CdTe
Strengths
Easy to produce
Cheapest PV you can buy
Main competitor to silicon
Major improvements in recent years 16 20%
Weaknesses
Cd is toxic
Te is quite scarce

## Slide 20: Thin film - CdTe
These graphs - Wu – about 16.5%

## Slide 21: Thin film – amorphous silicon
Advantages
a-Si is a direct gap semiconductor! Dundee 1970’s
Problems
Its not stable
The efficiency is low
No longer in serious production
Pic from Miles 2007

## Slide 22: Thin film – microcrystalline silicon
Advantage
Low cost thin film silicon could revolutionise solar power
Disadvantage
Silicon is an indirect gap material and does not absorb well 
Need to use tricks to get it to work
Ref 5 Sai – uses honeycomb textured substrate

## Slide 23: Thin film – microcrystalline silicon
Ref 5 Sai – uses honeycomb textured substrate

## Slide 24: Dye
Strengths
Does not require high purity semiconducdtors
Potentially cheap to produce with simple equipment
Weaknesses
Liquid electrolyte causes instability
Efficiency seems to be stuck at just over 10%
More difficult to manufacture than expected

## Slide 25: Dye

## Slide 26: Organic
Image from L M Peter Royal Soc
Bulk heterojunction:
P3HT – e donor
C60 derivative – e acceptor
P3HT – poly-3-hexyl-thiophene
glass
Transparent conductor
PEDOT:PSS
Al electrode

## Slide 27: Organic
Advantages
Has potential for low cost
Disadvantages
Unstable – absorption is an antibonding transition
Low efficiency
Companies can’t make it pay

## Slide 28: Organic
R Service Science 2011

## Slide 29: Multi-junction III-V
http://phys.org/news/2011-11-sharp-solar-cell-worlds-highest.html
http://www.semiconductor-today.com/news_items/2013/JUN/SHARP_190613.html

## Slide 30: Multi-junction III-V
600 x concentration
~40% efficient
Has accurate tracking system
Needs direct sunlight
Pics from Circadian Solar Ltd &
http://www.laserfocusworld.com
Concentrator
Tracker

## Slide 31: Multi-junction III-V
Advantages
Very high efficiency
Can be used with tracking concentrator systems
Disadvantages
High cost

## Slide 32: Multi-junction III-V
Ref 32 Chiu 2014

## Slide 33: Multi-junction thin film silicon
Advantage
All-Si multijunction using
a-Si (1.7 eV)
Microcrystalline Si (1.1eV)
Disadvantage
Complex for the efficiency gained.

## Slide 34: “Notable Exceptions”

## Slide 35: CZTSS = Cu2ZnSn(SxSe1-x)4
World annual production tonnes/year
50 Winkler
Eg = 1.16 eV; Voc = 0.5 V
- a 57% shortfall (very poor)

## Slide 36: CZTSS

## Slide 37: Hybrid Perovskite
Advantages:
Possible cheap PV route
Got efficient very quickly
Disadvantages:
Unstable, hysteretic, contains Pb

## Slide 38: Other concepts

## Slide 39: Intermediate band cells
Conduction band
Valence band
Intermediate band

## Slide 40: Quantum dot cells
Rsc/ Univ Texas
ETH Zurich

## Slide 41: Nanowire PV
CdTe
TCO
CdS
foil