Lecture 3
Fundamental Limitations of Solar Cells
R. Treharne
Nov 5th 2014

---
L3
Key Question
Why can't a solar cell have a 100% efficiency?
(Or even close to 100%?)
You should be able to answer this question after this lecture

---
Lecture Outline
Black Body Radiation
Detailed Balance
The Shockley-Queisser Limit
Requirements for real physical systems
Review of real PV device efficiencies
Exceeding the SQ limit (funky solar)

---
Black Body Radiation
A black body absorbs all radiation regardless of frequency or angle of incidence.
A black body in thermal equilibrium emits radiation according to Planck's Law.

---
Planck's Law
Photon Flux – Number of photons of energy E per unit area per second
b( E )={ 2F }over{ h^{3}c^{2} }left( {E^{2}} over {e^{E/k_{B}T}-1}right )
Units – Number of photons of energy E per unit area per second

---
Planck's Law
Photon Flux density from a spherical black body
b( E )={ 2F }over{ h^{3}c^{2} }left( {E^{2}} over {e^{E/k_{B}T}-1}right )
Look familiar?
c.f. Ideal diode
Units – Number of photons of energy E per unit area per second

---
Planck's Law
Photon Flux – Number of photons of energy E per unit area per second
b( E )={ 2F }over{ h^{3}c^{2} }left( {E^{2}} over {e^{E/k_{B}T}-1}right )
What the heck is this?
Units – Number of photons of energy E per unit area per second

---
Planck's Law
F = %pi sin^{ 2 }{ %theta }
Geometrical factor
B
%theta_{ B }
A
Black body
F_{ A }=%pi
F_{ A }=%pi
F_{ B }=%pi sin^{ 2}(%theta_{B})

---
Irradiance
Irradiance - Emitted energy flux density
L(E) = Eb(E)
This is what solar spectrum data is measured in

---
Irradiance
Irradiance - Emitted energy flux density
L(E) = Eb(E)
This is what solar spectrum data is measured in
Power Density given by
P = int^{infty}_{0}L(E)dE

---
Irradiance
Irradiance - Emitted energy flux density
L(E) = Eb(E)
This is what solar spectrum data is measured in
Stefan-Boltzmann Law
Power Density given by
P = int^{infty}_{0}L(E)dE = %sigma_{ s }T^{ 4 }
%sigma_{ S }={2%pi^{ 5 }k_{B}^{ 4 }}over{ 15c^{2}h^{3} }
Stefan's constant

---
Detailed Balance
What are we doing?
Counting all photons going in
Counting all photons going out
Difference must be converted into electrical
(electrochemical potential)
Key Assumptions
Mobility of carriers is infinite
All absorbed photons promote electrons
Only one interface absorbs/emits – other side contacted to a “perfect reflector”

---
Detailed Balance
In equillibrium (i.e. in the dark)
ambient photon flux (thermal photons)
ba(E)
hypothetical solar absorbing material
perfect reflector
Ambient emits like black-body
b_{ a } = {2F_{a}} over {h^{3}c^{2}}left( {E^2} over {e^{E/k_{B}T_{a}}-1}right)
F_{ a } = %pi

---
Detailed Balance
In equillibrium (i.e. in the dark)
ambient photon flux (thermal photons)
ba(E)
Reflectance
Absorbance
Ambient emits like black-body
b_{ a } = {2F_{a}} over {h^{3}c^{2}}left( {E^2} over {e^{E/k_{B}T_{a}}-1}right)
j_{ab s} = q( 1-R(E) )a( E )b_{a}( E )
Absorbed ambient results in an
equivalent current density
F_{ a } = %pi

---
Detailed Balance
In equillibrium (i.e. in the dark)
ambient photon flux (thermal photons)
emitted photon flux
ba(E)
Reflectance
Absorbance
Ambient emits like black-body too
Can think of as current in opposite direction to jabs
j_{ab s} = q( 1-R(E) )a( E )b_{a}( E )

---
Detailed Balance

---
Two Level System
thermalisation
Conduction Band (empty)
spontaneous emission
hν > Eg
Eg
hν = Eg
Valence Band (full)
What sort of materials do we use for solar cells?
   Semiconductors
Why?
   Because they have a band gap!
No longer a perfect system because of:
   THERMALISATION

---
Key Point
THERMALISATION:
Photons with E > Eg promote carriers that relax to bottom of conduction band through scattering interactions with phonons (transfer of kinetic energy – heat!)
Absorbed photon with E > Eg achieves the same result as E = Eg
Thermalisation is the most dominant loss mechanism that limits the efficiency

---
Photocurrent
Photo-current is due to the net absorbed flux due to the sun.
Can calculate by integrating jabs over all photon energies:
J_{ SC} = q int^{ infinity }_{0 }C( E )( 1-R(E) )a( E )b_{ s }( E )dE
Probability that promoted carriers are collected to “do work”

---
Photocurrent
Photo-current is due to the net absorbed flux due to the sun.
Can calculate by integrating jabs over all photon energies:
J_{ SC} = q int^{ infinity }_{0 }C( E )( 1-R(E) )a( E )b_{ s }( E )dE
Probability that promoted carriers are collected to “do work”
LOOK FAMILIAR?
  This is the Quantum Efficiency (external)

---
Photocurrent
Photo-current is due to the net absorbed flux due to the sun.
Can calculate by integrating jabs over all photon energies:
J_{ SC} = q int^{ infinity }_{0 }C( E )( 1-R(E) )a( E )b_{ s }( E )dE
Probability that promoted carriers are collected to “do work”
LOOK FAMILIAR?
  This is the Quantum Efficiency (external)

---
Photocurrent
Photo-current is due to the net absorbed flux due to the sun.
Can calculate by integrating jabs over all photon energies:
J_{ SC} = q int^{ infinity }_{0 }C( E )( 1-R(E) )a( E )b_{ s }( E )dE
Probability that promoted carriers are collected to “do work”
LOOK FAMILIAR?
  This is the Quantum Efficiency (external)
J_{ SC } = q int^{ infinity }_{ 0 }QE( E )b_{ s }( E )dE
Now you know how to calculate JSC from an EQE curve (hint hint)

---
Photocurrent
In a perfect world:
C( E) = 1
and
R( E) = 0
therefore
so
J_{ SC}=q int^{ infinity }_{ E_{g} }b_{ s }( E)dE
In other words JSC is dependent only on the band gap of the material
(for a given spectrum)
QE(E )=a( E) = left lbrace stack { 1 # 0 } right none E geslant E_{ g } E<E_{ g }

---
Photocurrent
From last lecture

---
VOC
Is the VOC related to the band gap too? - Heck Yes!
Remember from diode equation
V_{ OC } = {nk_{ B }T} over { q }ln left ({{J_{SC}} over {J_{0}}+1 } right )
This is much more sensitive to Eg than JSC is.
Level of dark current with respect to V is directly related to rate of stimulated emission.
The rate of stimulated emission depends on the size of the chemical potential of carriers deltamu
For a semiconductor deltamu is equivalent (almost) to the band gap /q
From the detailed balance
J_{ 0 }={ q }over{ k_{B} } { 15 %sigma_{s} } over { %pi^{4} }T^{ 3 } int^{ infinity }_{ u } {{ x^{2} } over { e^{x}-1 }dx}
where
u= {E_{ G }} over {k_{ B}T }
http://www.sciencedirect.com/science/article/pii/0927024895800042

---
VOC
J0 decreases exponentially with respect to band gap

---
VOC
Therefore:
VOC increases with Eg

---
Limiting Efficiency
VOC
JSC

---
Limiting Efficiency
Max limit on efficiency ~ 33%, corresponds to a band gap of ~ 1.4 eV
This is non-negotiable (or is it?)
Why aren't record cells at the limit?
Will discuss other recombination losses in lecture 5

---
The perfect solar cell

---
The Sun (again)
The sun is a black body emitter with a temperature of 5760K
At its surface, the Power density is:
       PS = 62 MW m-2
what is the power density of the Sun's emitted radiation at the Earth's surface, PE?
P_{ E } = F_{ E } over F_{ S }P_{ S }
        ~ 1353 m-2

---
Beating the SQ limit
Tandem Cells
Multi-junctions
Concentrator PV
Hot Carrier solar cells
Down and up conversion

---
Beating the SQ limit

---
Tandem Cells
Tandem Cells
Why have one junction when you can have two?
GaAs/InGaP
T. Takamoto et. al. “Over 30% Efficient InGaP/GaAs tandem solar cells”, APL, 70 381 (1997)

---
Tandem Cells
Detailed balance calculations for two band gap system:
Maximum theoretical efficiency ~ 46%

---
Tandem Cells
Disadvantages of tandems based on III-V's
High precision fabrication required
Materials balance (tunnel junction)
High cost (materials + deposition)
Not practical for concentrator systems
Are there other strategies?

---
Tandem Cells
Inorganic/Organic Hybrid Tandems
Cheap
Easy to make (non-vacuum dep)
Can apply to existing Si technology
Watch this space
c-Si efficiency boosted by 20% (by using perovskites)

---
Multi-junctions
Why have two junctions when you can have three (or more)?
Ge/InGaAs/InGaP – Max η ~ 35%

---
Multi-junctions
S. P. Bremner et. al. Prog. PV. 16:225-233 (2008)

---
Concetrators
Increase photon flux increase efficiency
Theoretical prediction for two junction system @ T = 320K

---
Concentrators
Fresnel Lenses
200 – 300 suns
1 axis tracking

---
Concentrators
Parabolic Mirror Array
~ 500 suns
25kW output
2 axis tracking

---
Concentrators
44.7%!
Four junction cell based on III-V
Fraunhofer Institute

---
Concentrators
Disadvantages of concentrator PV
Need to deal with high Temperatures
i.e. cooling required
High installation cost
Need direct sunlight
Don't put one on your roof in UK.

---
Hot Carrier Solar Cells
Can we get the promoted carriers out before they thermalise?
Use “selective” contacts that allow “hot” carriers to be collected before they thermalise (picoseconds!) to bottom of C.B. through scattering with phonon modes

---
Hot Carrier Solar Cells
Advantages of Hot Carrier Solar Cells
Max efficiency ~63%
Disadvantages
They don't exist!
Completely Theoretical to date
Lots of computational DFT studies
Expect real devices soon!

---
Hot Carrier Solar Cells
WOW!
Real hot carrier device demonstrated this 2014
http://scitation.aip.org/content/aip/journal/apl/104/23/10.1063/1.4883648

---
Up and down conversion
Take Parts of the spectrum that are not used by the device and covert to wavelengths/energies that are. How?

---
Lecture Summary
Luminescent Dyes
Quantum Dots/nanowires
Aluminium dots on GaAs solar cell
“Lego Brick” Structure.
Plasmonic Enhancement
http://www.nature.com/srep/2013/131007/srep02874/full/srep02874.html

---
Lecture Summary