Lecture 5
Junctions!
R. Treharne
Nov 6th 2014

---
L5
Lecture Outline

---
Metal-Semiconductor
Schottky Junction
metal
SC (n-type)
qχ
qφn
qφm
EC
EF
EG
EV
EV

---
Metal-Semiconductor
One Rule!
Fermi level must be in equilibrium
metal
SC (n-type)
qχ
qφn
EC
EG
EV
EV
qφm

---
Metal-Semiconductor
“Intimate Contact”
metal
SC (n-type)
metal
SC (n-type)
qχ
qφn
qχ
qφn
EC
EC
EG
EG
EV
EV
EV
EV
qφm
qφm

---
Metal-Semiconductor
BAND BENDING!
metal
SC (n-type)
metal
SC (n-type)
qχ
qφn
qχ
qφn
qVbi
EC
qφB
EC
EG
EG
EV
EV
EV
EV
“Built-in Voltage”
Vbi = φm - φs
φB = φm - χ
Barrier Height
qφm
qφm

---
Metal-Semiconductor
metal
SC (p-type)
qχ
qφp
qφm
EC
EG
EV
EV

---
Metal-Semiconductor
metal
SC (p-type)
metal
SC (p-type)
qχ
qφp
qχ
qφp
EC
qφm
EC
EG
EG
qφB
EV
EV
qVbi
EV
EV
Vbi = φm - φp
φB = EG/q - (φm - χ)
qφm

---
Metal-Semiconductor
φB = φm - χ
Why doesn't this rule hold?
Metal – SC interface effects
Lattice Mis-match
High density of defects
Interface states in gap

---
Semiconductor-Semiconductor
p-n homojunction
p
n
qχp
qχn
qφp
qφn
EC
EG
EG
EV

---
Semiconductor-Semiconductor
p-n homojunction
p
n
qχp
qχn
qφp
qφn
EC
EG
EG
EV

---
Semiconductor-Semiconductor
p-n homojunction
p
n
p
n
qχp
qφp
qχp
qχn
qφp
qφn
qχn
EC
qφn
EC
EG
EC
EG
EG
EV
EG
EV
EV

---
Semiconductor-Semiconductor
p-n homojunction
p
n
p
n
qχp
qχn
qφp
qφn
qVbi
EG
EG
EV

---
Semiconductor-Semiconductor
p-n homojunction
p
n
p
n
qχp
qχn
qφp
qφn
qVbi
Ei
EG
EG
Ei
EV

---
Semiconductor-Semiconductor
Defining Electrostatic potential, Ψ, for a SC
Difference between Ei and Ef
p-n homojunction
p
n
p
n
qχp
qχn
qφp
qφn
qVbi
Ei
qΨp
EG
EG
qΨn
Ei
EV
Vbi = Ψn - Ψp
KNOW HOW TO DRAW THIS!
Coming back here shortly to get a more physical picture
Electrostatic Potential, Ψ
Electron energy, E

---
Semiconductor-Semiconductor
Everybody's favourite homojunction - Silicon
Extrinsically doped
Every bit of electronics you own is jam packed with silicon homojunctions
p-type
n-type
iPhone 5:
1 billion transistors!
~ 45 nm wide
Mono-C solar cells
~750 μm thick
cell size = 1 cm2
http://electronics.howstuffworks.com/diode1.htm

---
Semiconductor-Semiconductor
p-n heterojunction: Different band gaps
1. Align the Fermi level. Leave some space for transition region.
p
n
qχp
qχn
qφp
qφn
ΔEC
EFn
EFp
ΔEV
narrow gap
wide gap

---
Semiconductor-Semiconductor
p-n heterojunction: Different band gaps
2. Mark out ΔEC and ΔEC at mid-way points
p
n
qχp
qχn
qφp
qφn
ΔEC
ΔEC
EFn
EFp
ΔEC
ΔEV
narrow gap
wide gap

---
Semiconductor-Semiconductor
p-n heterojunction: Different band gaps
3. Connect the C.B. and V.B. keeping the band gap constant in each material
p
n
Difference in band gaps give rise to discontinuities in band diagrams. This limits the carrier transport by introducing potential barriers at the junction
qχp
qχn
qφp
qφn
ΔEC
EFn
EFp
ΔEV
narrow gap
wide gap
Barrier to hole transport

---
Semiconductor-Semiconductor
Examples of p-n heterojections
Most thin-film PV technologies
http://pubs.rsc.org/en/content/articlehtml/2013/ee/c3ee41981a#cit111

---
Semiconductor-Semiconductor
Examples of p-n heterojections
III-V multi-junction devices
Being able to control the band offsets of a material can help eliminate barriers

---
Physical Picture
Drawing band schematics for junctions all day is fun, but what is actually going on here?
http://www.youtube.com/watch?v=JBtEckh3L9Q
Excellent qualitative description
6:27 – Didactic Model of Junction formation

---
Physical Picture
Equilibrium Fermi Levels – Explained – our one rule for drawing band schematics!
In thermal equilibrium, i.e. steady state: not net current flows
notice position of “metallurgical” junction. Usually call this x=0
J = J( drift)+J( diffusion) = 0
http://en.wikipedia.org/wiki/File:Pn-junction-equilibrium.png

---
Physical Picture
Lets look at hole current first:
matrix{ alignr J_{p} # {}={} # alignl J_{p}( drift)+J_{p}( diffusion) ## alignr {} # {}={} # alignl q%mu_{ p }p %xi -qD_{ p} { dp }over{ dx } }

---
Physical Picture
Lets look at hole current first:
matrix{ alignr J_{p} # {}={} # alignl J_{p}( drift)+J_{p}( diffusion) ## alignr {} # {}={} # alignl q%mu_{ p }p %xi -qD_{ p} { dp }over{ dx } }
hole distribution:
e-field:
diffusion coefficient
mobility:
%mu_{ p } = {e%tau} over {m_{ h }}
%xi = { 1 } over { e } { dE_{i} } over { dx }
p = n_{ i }e^{( E_{i}-E_{F} )/k_{B}T}
D_{ p} = ( k_{B}T/e )%mu_{ p }
Einstein relation
OK to use Boltzmann as approx to Fermi-Dirac
{dp} over {dx} = {p} over { k_{B}T } left ( {dE_{i}} over {dx} - {dE_{F}} over {dx} right)
will use this shortly

---
Physical Picture
matrix{ alignr J_{p} # {}={} # alignl J_{p}( drift)+J_{p}( diffusion) ## alignr {} # {}={} # alignl q%mu_{ p }p %xi -qD_{ p} { dp }over{ dx } ## alignr {} # {}={} # alignl %mu_{ p}p {dE_{i}} over {dx} - %mu_{ p}p left ( {dE_{i} over {dx}-{dE_{F}} over {dx}}right) ## alignr {0} # {}={} # alignl %mu_{ p}p { dE_{F} } over { dx } }
Condition for steady state

---
Physical Picture
TA DA!
{ dE_{F} over dx } = 0
The same is true from consideration of net electron current, Jn

---
Ideal Homojunction
p
n
qVbi
Ei
qΨp
qΨn
Vbi = Ψn - Ψp
Ei

---
Abrupt Junction
outside depletion region:
p = NA and n = ND
charge density
Space-charge condition
NAwp = Ndwn
i.e. areas of rectangles must be the same
electric field
Max field (at x=0):
ξm = qNDxn/εs = qNAxp/εs
Area = Vbi
ξm
V_{ bi } = %phi_{ n }-%phi_{ p} = {k_{ B }T} over q ln left( {N_{A}N_{D}} over {n_{i}^{2}} right )
electrostatic
potential
I've already called this Vbi
Hook & Hall, “Soild State Physics”, 2nd ed. Chap 6, p. 171

---
Abrupt Junction
outside depletion region:
p = NA and n = ND
charge density
Space-charge condition
NAwp = Ndwn
i.e. areas of rectangles must be the same
electric field
Max field (at x=0):
ξm = qNDxn/εs = qNAxp/εs
Lets derive this!
(but skip if I'm being slow)
Area = Vbi
ξm
V_{ bi } = %phi_{ n }-%phi_{ p} = {k_{ B }T} over q ln left( {N_{A}N_{D}} over {n_{i}^{2}} right )
electrostatic
potential
I've already called this Vbi
Hook & Hall, “Soild State Physics”, 2nd ed. Chap 6, p. 171

---
Abrupt Junction
From Earlier:
matrix{ alignr %phi # {}={} # alignl -{1 over e}(E_{i}-E_{F}) }
What is in p and n regions away from junction?
%phi
Here
p = n_{ i }e^{( E_{i}-E_{F} )/k_{B}T}
n = n_{ i }e^{( E_{i}-E_{F} )/k_{B}T}
and
left none %phi_{p} equiv-{1 over e}(E_{i} - E_{F}) mline {}_{x leslant -x_{p}} right none = -{ {k_{B}T} over e }left (N_{A} over n_{i} right )
S. M. Sze, “Semiconductor Devices: Physics and Technology”, Chap 4, p.90
left none %phi_{n} equiv-{1 over e}(E_{i} - E_{F}) mline {}_{x geslant -x_{n}} right none = -{ {k_{B}T} over e }left (N_{D} over n_{i} right )

---
Abrupt Junction
Hence:
V_{ bi } = %phi_{ n }-%phi_{ p} = {k_{ B }T} over q ln left( {N_{A}N_{D}} over {n_{i}^{2}} right )
How do I calculate in the depletion region? Must solve Poisson's Equation
%phi